
TENDER / MATERIAL SUBMITTAL INFORMATION
	
	

	Project Name
	______________________________________________

	Client
	______________________________________________

	Contractor
	______________________________________________

	Project Location / Site
	______________________________________________

	Tender Reference No.
	______________________________________________

	Specification Section
	______________________________________________

	Submission Date
	______________________________________________

	Prepared By
	______________________________________________


	Description
	Model Name
	Gap Size
	Image

	Supply and apply Pinnacle PFT gasketed Series floor-to-floor joint cover system designed for interior applications and suitable for use with most floor finishes where frame depth and configuration may vary to suit the selected finish material. The system consists of durable extruded aluminum frames paired with a TPR dual-durometer seal, ensuring reliable performance under building movement. All aluminum components are provided with a protective ZiO/ZnCrO₄ coating on surfaces in contact with surrounding finishes for enhanced corrosion resistance. The base frame is manufactured from extruded aluminum alloy 6063-T5, compliant with ASTM B221, while the gasket is formulated to 65 Shore A and 90 Shore A, conforming to ASTM D2000. The system is movement-tested by ensuring suitability for interior floor expansion joint applications. The PFT model is engineered to accommodate ±30% movement, providing dependable long-term performance across variable floor conditions.

	PFT 
	25-50 mm
	[image: image1.png]






Source: Pinnacle Solutions, 201/A, Arihant Royale, Shastri Nagar,Lal Bahadur Road, Mulund (W), Mumbai – 400080, Web: www.pinnaclesolutions.inTel.: +91-8108168086,E-mail: info@pinnaclesolutions.in

